11

RELATIVE HUMIDITY INDUCED REVERSIBLE HYDRATION OF SULFATE-INTERCALATED LAYERED DOUBLE HYDROXIDES 
S. RADHA1, K. JAYANTHI1, JOSEF BREU2,*, AND P. VISHNU KAMATH1,* 
1 Department of Chemistry, Central College, Bangalore University, Bangalore-5600 01, India

2 Department of Inorganic Chemistry I, University of Bayreuth, Bayreuth, Germany.

Running Title: HUMIDITY-INDUCED REVERSIBLE HYDRATION

*Authors for correspondance

 josef.breu@uni-bayreuth.de (J. B), vishnukamath8@hotmail.com (PVK),  

SUPPORTING INFORMATION
SI. 1. Observed 2θ values of [Zn-Cr-SO4] LDH at different relative humidities with the corresponding indices obtained using PROSZKI.
	Ambient

a = 3.11 Å

c = 8.93 Å

FM = 61.2
	0 % RH

a = 3.11 Å

c = 25.65 Å

FM = 24.3
	10 % RH

a = 3.13 Å

c = 8.95 Å

FM = 55.2
	100 % RH

a = 3.12 Å

c = 32.7 Å
FM = 23.0

	2θ(obs)
	hkℓ
	2θ(obs)
	hkℓ
	2θ(obs)
	hkℓ
	2θ(obs)
	hkℓ

	9.8

19.8

30.0

33.0

34.5

38.9

45.3

53.2

59.0

60.0

63.02
	001

002

003

100

101

102

103

104

110

111

112


	10.1

20.5

33.24

33.79

36.0

37.52

43.71

51.6

59.23

60.24

63.40
	003

006

101

012

104

015

018

0111
110

113

116


	9.8

19.8

30.0

33.0

34.4

38.9

45.3

53.1

59.0

60.0

63.0
	001

002

003

100

101

102

103

104

110

111

112


	8.0

16.1

24.3

33.4

34.8

35.8

38.2

39.8

43.3

45.1

51.5

59.0

59.7

61.6
	003

006

009

012

104

015

107

018

1010
0111
0114

110

113

116


[image: image1.wmf]0

20

40

60

80

100

8.0

8.5

9.0

9.5

10.0

10.5

11.0

11.5

0

10

20

30

40

50

60

70

80

90

100

110

8.0

8.5

9.0

9.5

10.0

10.5

11.0

11.5

0

10

20

30

40

50

60

70

80

90

100

110

8.0

8.5

9.0

9.5

10.0

10.5

11.0

11.5

0

10

20

30

40

50

60

70

80

90

100

110

8.0

8.5

9.0

9.5

10.0

10.5

11.0

11.5

0

20

40

60

80

100

8.0

8.5

9.0

9.5

10.0

10.5

11.0

11.5

 

 

 Dehydration cycle

 Hydration cycle

Basal spacings 

(

   

)

Relative humidity (%)

Å

[image: image2.png]


SI. 2. Basal spacing variation during humidity driven reversible hydration-dehydration of the (a) [Zn-Cr-SO4] LDH, and (b) [Zn-Al-SO4] LDH.

[image: image3.png]


[image: image4.wmf]0

20

40

60

80

100

8.5

9.0

9.5

10.0

10.5

11.0

 Hydration cycle

Basal spacing (Å) 

Relative humidity (%)

 Dehydration cycle


[image: image5.wmf]0

20

40

60

80

100

8.0

8.5

9.0

9.5

10.0

10.5

11.0

11.5

0

10

20

30

40

50

60

70

80

90

100

110

8.0

8.5

9.0

9.5

10.0

10.5

11.0

11.5

0

10

20

30

40

50

60

70

80

90

100

110

8.0

8.5

9.0

9.5

10.0

10.5

11.0

11.5

0

10

20

30

40

50

60

70

80

90

100

110

8.0

8.5

9.0

9.5

10.0

10.5

11.0

11.5

0

20

40

60

80

100

8.0

8.5

9.0

9.5

10.0

10.5

11.0

11.5

 

 

 Dehydration cycle

 Hydration cycle

Basal spacings 

(

   

)

Relative humidity (%)

Å

SI. 3. Schematic representation of the structural transformations occurring during hydration-dehydration of [Zn-Cr-SO4] LDH as a function of relative humidity.
SI. 4. Observed 2θ values of [Zn-Al-SO4] LDH with the corresponding indices obtained using PROSZKI.
	 (Ambient)

a = 5.34 Å
c = 11.14 Å

FM = 23.39
	10% RH
a = 3.06 Å

c = 25.77 Å

FM  = 18.6

	2θ
	hkℓ
	2θ
	hkℓ

	8.0

16.0

19.2

20.8
24.1

33.6

34.5

37.3

41.7

47.2

53.1

53.6

60.0

60.6

62.5


	001

002

100

101

003

110

111

112

113

114

211

115

300

301

302
	10.3
20.4
33.7
34.5

38.1

44.1
60.2
61.2
64.4
	003

006

101

012

015

018

110

113

116


SI. 5. Structure of the cation ordered [Zn-Al-SO4] LDH.

[image: image6.png]0% RH 10%RH
89A-1H ————» 86A-3Re— goi_1H
Ambient

10% RH

0% RH.
0% RH

1094-3R——»114-3R————» 109 4-3R,
1007 RH v RH




[image: image7.png]100%RH 100%RH

108A-17 11A-12 1A-17
0%R8
106417 Hoess

mmw

Biphasic s
104418 Pty @S
wirs]

994
Randomly interstcatified phase o

3nsﬂnT
ot ot

L SY N AU Y Y

Biphasict
(65T 00 ke prame)



SI. 6.    The structure of single layer cation ordered [Zn-Al-SO4] LDH viewing down the c-crystallographic axis. 
SI. 7. Result of the Rietveld refinement of cation ordered [Zn-Al-SO4] LDH.
	LDH
	Crystal System
	Space

Group
	Cell Parameters/Å
	Volume

/Å3
	Data Points
	Rwp
	Rp
	Rexp
	R(F2)
	χ2

	[Zn-Al-SO4]
	Hexagonal
	P-3
	a = 5.3488 (5)
c = 11.1537 (10)
	273.92
	4249
	0.141
	0.109
	0.04
	0.146
	3.50


SI. 8. Refined atomic position parameters of [Zn-Al-SO4] LDH.
	Atom
	Site
	x
	y
	z
	SOF

	Zn

Al

O​1

S

Oa
Ob
Ow
	2d

1a

6g

2c

2c

6g

6g
	0.6667

0.0000

0.0152

0.0000

0.0000

0.0782

0.5957
	0.3333

0.0000

0.2894

0.0000

0.0000

0.3342

0.8163
	0.0000

0.0000

0.0860

0.3583

0.4850

0.3256

0.5902
	0.3340

0.3351

0.3340

0.0867

0.0852

0.2395

0.0886


SI. 9. Refined bond distances and bond angles of the [Zn-Al-SO4] LDH.
	Distances (Å)
	Angles (°)

	Zn-O1

Zn-O1

Al-O1

S-Oa

S-Ob

S-Ow

O1-O1

O1-O1

 O1-O1*

 O1-O1*
	2.21132(18)
2.11020(17)
1.78820(13)
1.41274(13)
1.66023(15)
1.96084(17)
2.945

2.397

3.490

3.232
	O1-Zn-O1

O1-Zn-O1

O1-Al-O1

O1-Al-O1

Oa-S-Ob

Ob-S-Ob
	102.566(4)
88.830(3)
93.897(5)
86.103(5)
102.705(2)
115.306(1)


* Non-bonded in-plane O1-O1 distances.

SI. 10. Schematic representation of the structural variations during hydration-dehydration cycle of [Zn-Al-SO4] LDH.


� EMBED PowerPoint.Slide.12  ���





(a)





(b)












Å







image1.wmf

0


20


40


60


80


100


8.0


8.5


9.0


9.5


10.0


10.5


11.0


11.5


0


10


20


30


40


50


60


70


80


90


100


110


8.0


8.5


9.0


9.5


10.0


10.5


11.0


11.5


0


10


20


30


40


50


60


70


80


90


100


110


8.0


8.5


9.0


9.5


10.0


10.5


11.0


11.5


0


10


20


30


40


50


60


70


80


90


100


110


8.0


8.5


9.0


9.5


10.0


10.5


11.0


11.5


0


20


40


60


80


100


8.0


8.5


9.0


9.5


10.0


10.5


11.0


11.5


 


 


 Dehydration cycle


 Hydration cycle


Basal spacings 


(


   


)


Relative humidity (%)











